## Slide 1
Heterogeneous Catalysis
& Solid State Physics
Dohyung Kim
May 2, 2013
Physics 141A

## Slide 2
Catalysis
Catalysis : Increase in the rate of reaction due to a catalyst
Types of Catalysts
Homogeneous : Catalyst and Reactant in the same phase
Heterogeneous : Catalyst and Reactant in different phases
<http://www.chemguide.co.uk >

## Slide 3
Catalysis
Types of Catalysts
Homogeneous : Catalyst and Reactant in the same phase
e.g.) Organometallic Compounds
Heterogeneous : Catalyst and Reactant in different phases
e.g.) Metal Surface
<Cativa Process>
<Catalytic decomposition of formic acid on noble metals>
<International Journal of Hydrogen Energy Volume 37, Issue 21, 2012, 15956 - 15965>

## Slide 4
Heterogeneous Catalysis
Elementary steps in heterogeneous catalysis
Adsorption of reactants
Reaction of adsorbed intermediates
Desorption of products
Adsorptive property of a catalyst = Catalytic activity

## Slide 5
D-band Model(Chemisorption)
Electronic structure of transition metal
Interaction between energy levels
Adsorbate
Adsorbate
Broad band
Narrow band

## Slide 6
D-band Model(Chemisorption)
Formation of a chemical bond
<A. Nilsson et al., Chemical Bonding at Surfaces and Interfaces, Elsevier(2008)>
Antibonding
Bonding
Strong vs Weak chemisorption
Ed - EF
<B. Hammer et al., Advances in catalysis, Vol. 45(2000), 71-129>

## Slide 7
D-band Model(Chemisorption)
Variation in adsorption energies
Different Metal catalysts
ΔE(eV)
<B. Hammer et al., Advances in catalysis, Vol. 45(2000), 71-129>
# of d-electrons
Ed - EF

## Slide 8
D-band Model(Chemisorption)
Variation in adsorption energies
Different Facets
ex) FCC
Band Width(W) ~ sqrt(N)
Decreasing Atomic Density
<B. Hammer et al., Catalysis Letters, 46(1997), 31-35>
<A. Nilsson et al., Chemical Bonding at Surfaces and Interfaces, Elsevier(2008)>

## Slide 9
D-band Model(Chemisorption)
Variation in adsorption energies
Alloying
<J. R. Kitchin et al., J. Chem. Phys. 120, 10240 (2004)>
Control of reactivty through catalyst deposition
<A. Nilsson et al., Chemical Bonding at Surfaces and Interfaces, Elsevier(2008)>

## Slide 10
Volcano Curve
Plot of reaction rate vs property of a catalyst
(e.g. Heat of adsorption)
→ Volcano Shape
Sabatier Principle : The interaction between the
catalyst and the substrate should be “just right”
* Case of decomposition of formic acid on transition metals
<Karl Kochloefl (2005), "Heterogeneous Catalysis and Solid Catalysts“>
Activity related to various properties of a catalyst, mostly bulk properties.
The most fundamental parameter ?

## Slide 11
Bronsted-Evans-Polanyi(BEP) relation
Linear relationship between the activation energy
and dissociative chemisorption energy
Ea(=Ets) = aΔE + b
A2 + 2 * ↔ 2 A*
A2 + 2 *
2 A*
Ea
ΔE
Dissociative chemisorption energy determines the catalytic activity !
<Shengguan Wang et al., SLAC-PUB-14285>

## Slide 12
Simple Kinetic Models
Dissociative adsorption as RDS without strongly adsorbed A2
Dissociative adsorption as RDS with strongly adsorbed A2
Dissociative adsorption as RDS followed by rxn with strongly adsorbed B
* RDS : Rate-determining step
A2 + 2B ↔ 2AB

## Slide 13
Simple Kinetic Models
Dissociative adsorption as RDS without strongly adsorbed A2
※ Assumption : Coverage of A2 and B on the surface is negligible
Ex> Ammonia synthesis
Step 1 - A2 + 2* ↔ 2A*
Step 2 - A* + B ↔ AB + *
(* : active site)
A2 + 2 * + 2B
2 A* + 2B
2AB + 2 *
Ea
ΔE1
<T. Bligaard et al., Journal of Catalysis 224(2004), 206-217>
= Q/K)

## Slide 14
Simple Kinetic Models
Dissociative adsorption as RDS without strongly adsorbed A2
<T. Bligaard et al., Journal of Catalysis 224(2004), 206-217>
Choice of catalyst depends on deviation from equil.
More exothermic → Larger Keq → Smaller
→ Stronger dissociative chemisorption catalyst
<C. J. H. Jacobsen et al., Journal of Catalysis 205(2002), 382-387>
Optimal catalyst in ammonia synthesis

## Slide 15
Simple Kinetic Models
Dissociative adsorption as RDS without strongly adsorbed A
<T. Bligaard et al., Journal of Catalysis 224(2004), 206-217>
Dependence on T : modest
Low temp process for noble catalysts
(smaller )
Dependence on P : negligible

## Slide 16
Simple Kinetic Models
Dissociative adsorption as RDS with strongly adsorbed A
Step 1 - A2 + * ↔ A2*
Step 2(RDS) - A2* + * ↔ 2A*
Step 3 - A* + B ↔ AB + *
(* : active site)
A2 + 2 * + 2B
2 A* + 2B
2AB + 2 *
Ea1
ΔE2
ΔE1
A2* + * + 2B
<T. Bligaard et al., Journal of Catalysis 224(2004), 206-217>
2

## Slide 17
Simple Kinetic Models
Dissociative adsorption as RDS with strongly adsorbed A
<T. Bligaard et al., Journal of Catalysis 224(2004), 206-217>
2
larger than -1eV, negligible
smaller than -1eV, more reactive catalyst needed(stronger binding of A)

## Slide 18
Simple Kinetic Models
Dissociative adsorption as RDS followed by rxn with strongly adsorbed B
※ Assumption : Coverage B on the surface significant
Step 1(RDS) - A2 + 2* ↔ 2A*
Step 2 - B + * ↔ B*
Step 3 - A* + B* ↔ AB + 2*
(* : active site)
A2 + 4* + 2B
2 A* + 2* + 2B
2AB + 4*
Ea
ΔE1
2 A* + 2B*
2ΔE2
<T. Bligaard et al., Journal of Catalysis 224(2004), 206-217>
1
2
Competition of A & B

## Slide 19
Methanation
CO + 3H2 → CH4 + H2O
(1)
(2)
<T. Bligaard et al., Journal of Catalysis 224(2004), 206-217>
<T. Bligaard et al., Journal of Catalysis 224(2004), 206-217>
<M. A. Vannice, Journal of Catalysis 50(1977), 228-236>
-1.0 ~ -1.6eV

## Slide 20
Universality of BEP relation
<T. Bligaard et al., Journal of Catalysis 224(2004), 206-217>
<R. H. Anderson and M. Boudart, Catalysis: Science and Technology(1981), 87-158>
Ammonia Synthesis
-1.27eV
-0.38eV
-0.10eV
-0.84eV
-0.70eV
-0.59eV
1.37eV
NO reduction catalysis
Pt(-1.27eV) known to be one of the best catalysts

## Slide 21
Conclusions
Catalytic activity is dependent upon the adsorption of a reactant, which is determined by surface solid state of a catalyst
Dissociative chemisorption energy is the fundamental parameter leading to the Volcano Plot
BEP relation can be used to predict optimal catalysts for specific reactions in the same class